SECTION 05 53 00

METAL GRATINGS

Note to Specifier:  This section covers metal gratings fastened to support steel with Hilti Screw-in X-FCM Grating Fastening System.  Consult Hilti for assistance in editing this section for the specific application.

PART 1 – GENERAL

1.01	SUMMARY

- Section Includes:

  - Metal gratings fastened to support steel with screw-in grating fastening system

- Related Sections:

  - Section 051200 - Structural Steel

1.02	REFERENCES

A.	ANSI/NAAMM MBG 531 - Metal Bar Grating Manual

B.	ASTM A123 - Standard Specification for Zinc (Hot-Dip Galvanized) Coatings on Iron and Steel Products

C.	ASTM A153 - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware

D.	ASTM A510 - Standard Specification for General Requirements for Wire Rods and Coarse Round Wire, Carbon Steel

E.	ASTM A780 - Standard Practice for Repair of Damaged and Uncoated Areas of Hot-Dip Galvanized Coatings

F.	ASTM B221 - Standard Specification for Aluminum and Aluminum Alloy Extruded Bars, Rods, Wire, Profiles and Tubes

G.	ISO 9001 - Quality Management Systems -- Requirements

H.	ISO 14001 - Environmental Management Systems -- Specification with Guidance for Use

1.03	SUBMITTALS

A.	Comply with Section 01330 - Submittal Procedures

- Product Data:

- Submit grating manufacturer's product data including load tables.

- Submit fastener manufacturer's product data including installation instructions.

- Shop Drawings:  Submit grating manufacturer's shop drawings, indicating grating type, material, bearing bar size and spacing, cross bar spacing, top surface type, dimensions, tolerances, clearances, span, fabrication, shop welding, supports, toe plates, banding bars, cutouts, stair treads, finish, and location of fasteners.

- Samples:  Submit fastener manufacturer's samples of grating fasteners.

- Manufacturer's Certification:  Submit fastener manufacturer's certification indicating supplied grating fasteners comply with manufacturer’s published specifications.

1.04	QUALITY ASSURANCE

- Grating Fastener Manufacturer:  ISO 9001 and ISO 14001 certified company

- Grating Fasteners:  Lloyd’s Registered and ABS Type Approved

C.	Field Measurements:  Take field measurements before preparation of shop drawings and fabrication, as necessary.

1.05	DELIVERY, STORAGE, AND HANDLING

- Delivery:

1.	Gratings:  Deliver metal gratings to site with labels on each panel clearly identifying manufacturer, panel size and location of installation.

2.	Fasteners:  Deliver grating fasteners to site in manufacturer's original, unopened containers and packaging with labels clearly identifying product name and manufacturer.

- Storage:

1.	Gratings:  Store metal gratings flat, in clean, dry area, off ground in accordance with grating manufacturer's instructions.  Protect grating edges from damage.

2.	Fasteners:  Store grating fasteners in clean, dry area in accordance with fastener manufacturer's instructions.

C.	Handling:  Protect materials and finish from damage during handling and installation.

PART 2 – PRODUCTS

2.01	MANUFACTURERS

- Metal Grating Manufacturers:

1.	____________________

2.	____________________

3.	____________________

- Grating Fastener Manufacturer:

1.	Hilti, Inc., 7250 Dallas Parkway, Suite 1000, Plano, Texas 75024.  Toll Free (800) 879-8000.  Fax (800) 879-7000.  Technical Support (800) 879-6000 x6337.  Web Site www.us.hilti.com.

2.	Other manufacturers will not be allowed.

2.02	METAL GRATINGS

A.	General:  Manufacturing, fabrication, welding, and tolerances shall be in accordance with ANSI/NAAMM MBG 531.

B.	Type:  [Welded steel]  [Pressure-locked steel]  [Pressure-locked aluminum flush top]  [Pressure-locked aluminum rectangular bar]  [Pressure-locked aluminum I-Bar]   [____________________]

C.	Material and Finish:

1.	Steel:

a.	Bearing Bars:  ASTM A36

b.	Cross Bars:  ASTM A510

c.	Finish:  [Hot-dipped galvanized after fabrication, ASTM A123]  [Painted, 1 coat manufacturer's standard red or black paint]  [ ____________________ ]

2.	Aluminum:

a.	Bearing Bars:  ASTM B221, Alloy 6061-T6 or 6063-T6

b.	Cross Bars:  ASTM B221, Alloy 6061-T1

c.	Finish:  [Mill]  [Class I clear anodized]

3.	Stainless Steel:

a.	Finish:  Mill

Note to Specifier:  Specify bearing bar size and spacing.  Hilti Screw-in X-FCM Grating Fastening System can accommodate a grating depth of 1 to 2 inches.  Consult Hilti if a grating depth greater than 2 inches is required. The grating fastening system requires a minimum clear distance between bearing bars of 3/4 inch and a maximum bearing bar spacing of 1-3/16 inches on center.

- Bearing Bars:

1.	Depth:  [1 inch]  [1-1/4 inches]  [1-1/2 inches]  [1-3/4 inches]  [2 inches]  [ _____ inches]  [As indicated on the drawings]

2.	Thickness:  [1/8 inch]  [3/16 inch]  [ _____ inch]  [As indicated on the drawings]

3.	Spacing:  [1-3/16 inches on center]  [15/16 inches on center]  [ _____ inches on center]  [As indicated on the drawings]

E.	Cross Bar Spacing:  [4 inches on center]  [2 inches on center]  [ _____ inches on center]  [As indicated on the drawings]

F.	Top Surface:  [Plain]  [Serrated]  [Abrasive finish, aluminum oxide aggregate in epoxy resin adhesive]  [ ____________________ ]  [As indicated on the drawings]

- Toe Plates:

1.	Height:  [4 inches]  [ _____ inches]  [As indicated on the drawings]

2.	Attachment:  [Attach toe plates to gratings by welding in shop.]  [As indicated on the drawings.]

H.	Banding Bars:  Provide ends of grating panels and openings in gratings with banding bars of same material and height as gratings.

- Stair Treads:

1.	Same metal grating type, material, finish, bearing bars and top surface

2.	Nosings:  [Cast abrasive]  [Corrugated angle]  [ _______________ ]  [As indicated on the drawings]

2.03	GRATING FASTENERS

Note to Specifier:  There are a number of methods to secure metal gratings to support steel.  Only the Hilti Screw-in X-FCM Grating Fastening System is specified in this section.  The X-FCM Grating Fastening System consists of two components:  an 8 mm screw-in threaded stud (S-BT) and the X-FCM Grating Disk.  The S-BT-GR stud is SAE316 equivalent for corrosive environment applications.  The S-BT-GF stud is made from carbon steel with electroplated Zn-alloy coating for cathodic protection and a topcoat for chemical resistance (Duplex-coating) for mildly corrosive environment applications.  Consult Hilti for more information regarding these grating fastening systems.

- Fasteners:  Hilti Screw-in X-FCM Grating Fastening System.

1.	Grating Disks:  Assembly of 52 mm diameter disk and 8 mm internally threaded screw

a.	Carbon Steel:  SAE 1008.  Hot-dip zinc galvanized, ASTM A 153 to a minimum of 65 micrometers thickness

b.	Stainless Steel:  SAE 316 or equivalent

2.	Threaded Studs:  8 mm screw-in threaded studs fastened to support steel in field with Hilti cordless drill tools to pre-drill the hole and screw-in the threaded stud

Note to Specifier:  Specify Hilti S-BT-GF M8/7 AN6, S-BT-GR M8/7 SN6 or S-BT-GR M8/7 SN6 AL* screw-in threaded studs for hot-dip zinc galvanized carbon steel and stainless steel grating disks in applications where threaded stud fastener point will penetrate through support steel (support steel from 3mm to 6mm). Specify Hilti S-BT-GR M8/7 SN5 screw-in threaded studs for hot-dip galvanized carbon steel and stainless steel grating disks in applications where threaded stud fastener point must not penetrate through support steel (support steel from 5mm to 6mm).  Specify Hilti S-BT-GF M8/7 AN6, S-BT-GR M8/7 SN6 or S-BT-GR M8/7 SN6 AL* screw-in threaded studs for hot-dip galvanized carbon steel and stainless steel grating disks in applications where threaded stud fastener point must not penetrate through support steel (support steel minimum 6mm). Contact Hilti for more information on threaded studs.

*S-BT-GR M8/7 SN6 AL for use in aluminum base material

a.	Carbon Steel: Grade 1038 with duplex coating. The coating consists of an electroplated zinc alloy layer and a topcoat.

b.	Stainless Steel:  SAE 316 or equivalent

PART 3 – EXECUTION

3.01	EXAMINATION

A.	Examine support steel to receive metal gratings for correct size, layout and alignment.  Notify Engineer if supports are not acceptable.  Do not begin installation until unacceptable conditions have been corrected.

3.02	INSTALLATION - METAL GRATINGS

A.	Install metal gratings in accordance with grating manufacturer's instructions and ANSI/NAAMM MBG 531 at locations indicated on the drawings.

B.	Ensure support steel bearing surfaces are clean.

C.	Install gratings level, square, rigid, with flush installation and without warp.

D.	Install gratings with cross bars in alignment.

E.	Support grating panels on all sides and attach to support steel with a minimum of two fasteners per full-size panel width.

F.	Cut openings for penetrations accurately to size and location.

G.	Cut openings for pipes a minimum of 2 inches larger in diameter than pipe.

Note to Specifier:  Specify the following sentence for galvanized steel gratings.

H.	Repair damaged galvanized steel grating surfaces and apply galvanizing repair paint in accordance with ASTM A 780.

Note to Specifier:  Specify the following sentence for aluminum gratings.

I.	Protect aluminum grating surfaces from direct contact with dissimilar metals by painting dissimilar metal with 1 coat of bituminous paint or other approved insulating material.

J.	Replace defective or damaged gratings as directed by Engineer.

3.03	INSTALLATION - GRATING FASTENERS

A.	Install grating fasteners to clamp grating to support steel in accordance with fastener manufacturer's instructions.

B.	Fasten threaded studs to support steel using fastening tools provided by fastener manufacturer.

- Screw-in threaded studs into support steel to proper embedment depth in accordance with fastener manufacturer's instructions.

Note to Specifier:  S-BT screw-in threaded studs must be installed into pre-drilled holes (specific match-tolerance drill bit required) in the support steel. Contact Hilti for S-BT installation instructions.

E.	Fasten threaded studs perpendicular to support steel.

F.	Use proper grating disk length to accommodate grating depth.

G.	Tighten internally threaded screw of grating disk onto threaded stud with maximum tightening torque depending on thickness of support steel in accordance with fastener manufacturer's instructions.  Use tightening tool provided by fastener manufacturer.

H.	Install fasteners with a minimum thread engagement of 4 number of threads (5 mm) between grating disk internally threaded screw and threaded stud.

3.04	PROTECTION

A.	Protect installed metal gratings and fasteners from damage during construction.

END OF SECTION